## Slide 1: Performance Based Design of Exposed Mass Timber
Robert Dixon – robert.dixon@arup.com
Items to Consider
The Macallan Distillery, Easter Elchies

## Slide 2
The Macallan Distillery, Easter Elchies
Contents
Mass Timber
Design Intent
Technical Challenges
  Fire Resistance Levels
  Self-extinguishment
  Delamination
  Adhesives
  Connections
Non-Technical Challenges
Design Tools Available
New Eurocode 5
Some Performance Based Watch-its
Practical Design Measures

## Slide 3
The Macallan Distillery, Easter Elchies
Mass Timber
CLT – Cross Laminated Timber
layers of timber, known as lamellas, are glued together with the grain alternating at 90 degree angles for each layer.
Panels/slabs of timber
LVL – Lumber Veneer Lumber
manufactured by bonding together rotary peeled or sliced thin wood veneers under heat and pressure
Beams/columns/cassettes
Glulam – Glued Laminated Timber
comprises of a number of layers of timber bonded together with a moisture resistant adhesive or glue. Multiple smaller pieces are glued together to make one large strong beam.
Beams/columns

## Slide 4
The Macallan Distillery, Easter Elchies
Rather than…
Mass Timber

## Slide 5
The Macallan Distillery, Easter Elchies
Design Intent - What Does the Design Need to Achieve?
Architectural Intent - Exposed / Encapsulated / Both
Low-Rise
Accepted that a low rise building may be lost in a fire.
Mid-Rise
Maybe acceptable to lose in a fire, if occupant can escape and there is a demonstrated period for fire brigade intervention.
High-Rise
Occupants may be required to remain in the building.
Occupants may be above fire floor.
Takes fire brigade longer to intervene.
Structure must survive burn-out.
Risk

## Slide 6
The Macallan Distillery, Easter Elchies
Technical Challenges
Risk
(height, exposure, use)
Time
2013
2017
2018
Fully encapsulated.
Timber Timeline
Fully exposed.
<25m
Fully exposed.
>25m

## Slide 7
The Macallan Distillery, Easter Elchies
Technical Challenges
Fire Resistance Levels (global)
Is it reasonable to add fire load, and remove fire resistance?
Traditional time equivalence not applicable.
Structure contributes to fuel.

## Slide 8
The Macallan Distillery, Easter Elchies
Technical Challenges
Fire Resistance Levels (global)
More exposed timber, more fuel, longer duration.
Delaminating CLT, fire re-growth, unpredictable.
Higher required FRL.

## Slide 9
Fire Modelling – Exposed timber
Fuel load 500MJ/m2
Technical Challenges

## Slide 10
Fire Modelling – Exposed timber
Fuel load 750MJ/m2
Technical Challenges

## Slide 11
Fire Modelling – Exposed timber
Fuel load 1100MJ/m2
Technical Challenges

## Slide 12
The Macallan Distillery, Easter Elchies
Technical Challenges
Fire Resistance Level (element)
Fire Resistance = Char Rate x Exposure Time
  What is exposure time?
    Complete burnout in a high rise building.
    Burn duration increases with amount of exposed timber.
  What is char rate?
    Building specific.
    Timber specific.
    Exposure specific.
Applicability of standard fire tests for timber elements.

## Slide 13
The Macallan Distillery, Easter Elchies
Technical Challenges
Self-Extinguishment
Very influential factor in exposed timber design.

## Slide 14
The Macallan Distillery, Easter Elchies
Technical Challenges
Self-Extinguishment
Large variability design values applied;
  University of Queensland (Emberley et al.) - 45kW/m2
  Delft University (Crielaard) - 6kW/m2
Has a huge impact on the design;
  Fire duration, delamination, size and intensity of fire, char rates.
  Fire Resistance Level.
How compatible are the tests to a specific building?
  Fuel load, ventilation, surface air flow, compartment size.

## Slide 15
The Macallan Distillery, Easter Elchies
Technical Challenges
Delamination (char fall-off)
Inhibits self-extinguishment. Promotes fire re-growth
Influences duration, char rate and Fire Resistance Level
FPRF tests; single wall exposure

## Slide 16
Delamination – Fire re-growth
Technical Challenges
Fire Protection Research Foundation (NRCC and SP), Test at NIST: Test 1-4

## Slide 17
The Macallan Distillery, Easter Elchies
Technical Challenges
Adhesives (CLT)
Choice of adhesive impact fire performance of CLT.
High temperature adhesives can reduce / eliminate delamination.

## Slide 18
The Macallan Distillery, Easter Elchies
Technical Challenges
Connections
Connections should undergo a loaded fire test.
Otherwise sophisticated analytical approach required.
Increased charring at connections.
Not all fire tests are loaded.

## Slide 19
The Macallan Distillery, Easter Elchies
Technical Challenges
Encapsulation Failure
If timber is not encapsulated or protected properly, then elements becomes exposed.
Elements behind failed encapsulation may not be designed to char.
Encapsulation failure can be encompassed within the system design, underpinned by compatible test data.
Image from: Zelinka, Samuel L.; Hasburgh, Laura E.; Bourne, Keith J.; Tucholski, David R.; Ouellette, Jason P. (In press). Compartment fire testing of a two-story cross laminated timber (CLT) building. General Technical Report FPL-GTR-247. Madison, WI: U.S. Department of Agriculture, Forest Service, Forest Products Laboratory.

## Slide 20
The Macallan Distillery, Easter Elchies
Non-Technical Challenges
Testing vs Analysis
Fire engineers need to be aware of the risk they are taking on when undertaking non-validated analysis.
Often there is pressure to undertake assessment in lieu of testing.
Much of our work is outside (or beyond) the scope of codes.

## Slide 21
The Macallan Distillery, Easter Elchies
Non-Technical Challenges
Early Fire Engineering Input Required
Due to procurement process, structural elements need to be fully designed much earlier in the project cycle.
Early engagement with architect, structures, acoustics and building services is key to project success.
Testing schedule should be defined early as to not impact program.

## Slide 22
The Macallan Distillery, Easter Elchies
Design Tools - Char Model for Delaminating CLT
  Pros
  Offers methodology to determine element FRL for delaminating CLT (not previously available).
  Quick, easy to use.
  Solid theoretical basis.
  Cons
  Relies on initial nominal char rate input.
  Not embodied in a current code.
Eurocode 5 proposed method |  |  |  |  | 
(From "Design of Cross-Laminated Timber in Fire", by Klippel and Schmid, ETH) |  |  |  |  | 

## Slide 23
The Macallan Distillery, Easter Elchies
Design Tools - Parametric Fire Curves
  Pros
  Quick, inexpensive.
  Accepted within academic community and approval authorities.
  Can be used to determine FRL and burn duration.
  Cons
  Only applicable to smaller compartments.
  Difficult to allow for char fall-off.
  Limited validation.
Chart: Char rates under ISO 834 and Eurocode 1 Parametric Fires

## Slide 24
The Macallan Distillery, Easter Elchies
Design Tools - FDS / Pyrolysis Simulation
  Pros
  Accurate representation of timber burning characteristics.
  Large compartment application.
  Good validation for small (cone calorimeter) and medium scale (room tests).
  Cons
  Very time consuming.
  Computationally expensive.
  No validation for large scale (e.g. open plan compartments).
  Can be costly.
  More suited to research at the moment.

## Slide 25
The Macallan Distillery, Easter Elchies
Design Tools – Finite Element Modelling
  Pros
  Potentially accurate representation of heat transfer through timber.
  Can be used to determine loadbearing capacity of elements, connections or frames.
  Cons
  Timber material models can be very complex.
  Significant and potentially complex validation required.
  Computationally expensive.
  Costly.

## Slide 26
The Macallan Distillery, Easter Elchies
New Eurocode 5 (BS EN 1995-1-2)
Currently out for public review. Revision includes;
Improved charring and ‘effective cross section’ models.
Simplified calculation for failure of plasterboards included.
CLT is covered more specifically.
Improved design rules for connections, now up to 90 mins.
Still to be developed;
Testing standards for insulation and glue performance.

## Slide 27
The Macallan Distillery, Easter Elchies
Performance Based Watch-its
  Fire testing and fire dynamics has shown that more exposed timber – more fuel, longer fire, higher char rates, higher required Fire Resistance.
  Delaminating CLT – regrowth can lead to a very long and unpredictable fire. Adhesive dependent. CLT can only be designed to have predictable compartment response if the adhesives does not cause delamination.
  No validation for fire dynamics within a large compartment containing exposed timber surfaces.
  Research and test data should be used in the correct context e.g. UQ self-extinguishment demonstration should not be used as the basis for building design.
  Undertake analytical assessments with caution.

## Slide 28
The Macallan Distillery, Easter Elchies
Practical Design Measures
Consider amount and location exposed timber.
High temperature / PUR adhesives for CLT.
Thick exposed lamella for CLT.
Configure compartments for favourable ventilation conditions.
Holistic design (e.g. improved sprinkler reliability / egress systems etc.)
Project specific testing.

## Slide 29: Thank you
The Macallan Distillery, Easter Elchies